## Slide 1: Exploring the Nanoworld with Small-Angle Scattering
Dale W. Schaefer
Chemical and Materials Engineering Programs
University of Cincinnati
Cincinnati, OH 45221-0012
dale.schaefer@uc.edu
Braggs Law and wave interference
Why do Small-Angle Scattering?
Imaging vs. Scattering
Basic Concepts
  Scattering Vector, Fourier Trns.
  Scattering Length Density
Particle Scattering
  Guinier Approximation
  Porod’s Law
Fractal Structures
Nanocomposites
SAXS & SANS: θ ≤ 6°
XRD
SAS
Source of x-rays, light or neutrons

## Slide 2: Crystals: Bragg’s Law and the scattering vector, q
θ
d
Ordered Structures give peaks in “reciprocal” Space.
Large structures scatter at small angles.
The relevant size scale is determined by 2π/q
q is a vector.
You can’t always determine the real space structure from the scattering data.
Problem: Nanomaterials are seldom ordered
SAXS: θ < 6°
real space
source
detector
Reciprocal space
Notes: "square" is related to the "phase problem." Not really a problem. For ordered systems we want to know the real-space structure. Not necessarily true for disordered systems.
Bragg's law includes a vector. Pole parallel to q.

## Slide 3: Disordered Structures in “Real Space”
10µm
Agglomerates
Primary Particles
Aggregates
Precipitated Silica
(NaO) (SiO2)3.3 + HCl —> SiO2 + NaCl
10 nm
Water Glass
Complex
Hierarchical
Disordered
Difficult to quantify structure from images.
Notes: We don't really want to know all the positions.

## Slide 4: Hierarchical Structure from Scattering
100,000 nm
200 nm
0.5 nm
10 nm
Agglomerate
Aggregate
Primary
Particle
Network
“Polymer”
Four Length Scales
Four Morphology Classes
Exponents related to
morphology
10
-7
10
-6
10
-5
0.0001
0.001
0.01
0.1
1
10
Intensity
-4.0
-2.0
-3.1
R
G
= 89
μ
q [Å-1] ~ Length-1 ~ sin(θ/2)
USAS
SAS
Real
Space
Reciprocal
Space

## Slide 5: Why Reciprocal Space?
10 µm
Isotactic polystyrene foams prepared by TIPS
Jim Aubert, SNL
Ultra-small-angle neutron scattering: a new tool for materials research. Cur. Opinion Sol. State & Mat Sci, 2004. 8(1): p. 39-47.
Images miss similarity

## Slide 6: Adding up the Phases
r2
r3
r4
Electron density distribution
n(r) = number of electrons in a volume element dr = dx dy dz around point r.
Scattering length density distribution
ρ(r) = scattering length in a volume element dr = dx dy dz around point r.
ρ(r) = bn(r)
Many electrons
Amplitude is the Fourier transform of the SLD distribution (almost)
r1
scattering length of one electron
Notes: 1 occurs because one particle is at the Origin, which need not be the case.

## Slide 7: Scattering Length Density (SLD) Distribution
Fourier transform of
the scattering length
density distribution
Can’t be measured
ρ(r)
What we measure: Square of the Fourier transform of the SLD distribution
Can’t be inverted

## Slide 8: Characterizing Disordered Systems in Real Space
r
Real space
ξ
Electron Density Distribution
Correlation Function of the
Electron Density Distribution
Depends on latitude and longitude.
Too much information to be useful.
Depends on separation distance.
Retains statistically significant info.
r
Resolution problems at small r
Opacity problems for large r
2-dimensional
Operator prejudice
Throw out phase information
×
Problems with real space analysis
Notes: It would be difficult to live in a world where eyes were sensitive to phase. Be careful what you wish for.

## Slide 9: Imaging vs. Scattering
r
q
Real space
Reciprocal space
ξ
ξ-1
Schaefer, D. W. & Agamalian, M. Ultra-small-angle neutron scattering: a new tool for materials research. Curr Opin Solid St & Mat Sci 8, 39-47, (2004).
Pegel, S., Poetschke, P., Villmow, T., Stoyan, D. & Heinrich, G. Spatial statistics of carbon nanotube polymer composites. Polymer 50, 2123-2132, (2009).

## Slide 10: Scattering from Spherical Particle(s)
2R
ρo
v = particle volume
I(q) ~ N(ρ - ρo)2v2P(q)
solvent SLD
Form Factor
N particles
Notes: ----- Meeting Notes (3/17/12 17:23) -----
Which cross section is this? What are the Units
----- Meeting Notes (3/17/12 17:29) -----
I(0) very sensitive to the large particles. Based on Bragg principles where would small particles show up.

## Slide 11: Particles in Dilute Solution
ρ1
ρ2
RV
R
1 particle

## Slide 12: Small-Angle Scattering from Spheres
Large object scatter at small angles
Silica in Polyurethane
AFM
Guinier Regime
Porod (power-law) Regime
Diameter = 140 Å
3 mm
Petrovic, Z. S. et al. Effect of silica nanoparticles on morphology of segmented polyurethanes. Polymer 45, 4285-4295, (2004)

## Slide 13: Guinier Radius
Initial curvature is a measure of length
Rg ~ 1/q
Derived in 5.2.4.1
Notes: Rg = moment of inertia

## Slide 14: Guinier Fits
Notes: Logx =(ln x)/2.303
print (ln(360)-ln(50))/9.5e-4
2077.98
print sqrt(3*2077)
79 Å

## Slide 15: Dense packing: Correlated Particles
Packing Factor = k = 8 ϕ
Packing Factor ≅ 6
ξ
R
Å
Å
Notes: ----- Meeting Notes (3/17/12 17:44) -----
Calculation in Extras

## Slide 16: Colloidal Silica in Epoxy
50 nm
Exclusion zone
EPON 862 + Cure W+ Silica
Chen, R.S. et al, Highly dispersed nanosilica-epoxy resins with enhanced mechanical properties Polymer, 2008. 49(17): p. 3805-3815.
Notes: The composite matrix analyzed in this work is Epon 862 epoxy
resin (diglycidyl ether of bisphenol F epoxy, Shell Corporation)
cured with EpiCure-W(diethyl diamino toluene, Shell Corporation).
Both materials were purchased from Miller-Stephenson Chemical
Company, Inc. In the remainder of this work, we refer to the cured
epoxy system (epoxy ?cure agent) as Epon862/W. This resin system
has been studied for aerospace applications due to its high
working temperature, good properties, and low viscosity [27].
These properties are all significant when resin-transfer molding
advanced carbon-fiber-reinforced composites.

## Slide 17: Using RG: Agglomerate Dispersion
Light Scattering
sonicate
hard agglomerate
dry
3.5 µm
D.W. Schaefer, D. Kohls and E. Feinblum, Morphology of Highly Dispersing Precipitated Silica: Impact of Drying and Sonication. J Inorg Organomet Polym, 2012. 22(3): p. 617-623.)

## Slide 18: Beyond RG: Hierarchical Structure from Scattering
100,000 nm
200 nm
0.5 nm
10 nm
Agglomerate
Aggregate
Primary
Particle
Network
“Polymer”
Four Length Scales
Four Morphology Classes
Exponents related to
morphology
10
-7
10
-6
10
-5
0.0001
0.001
0.01
0.1
1
10
Intensity
-4.0
-2.0
-3.1
R
G
= 89
μ
q [Å-1] ~ Length-1 ~ sin(θ/2)
USAXS
SAXS

## Slide 19: Mass-Fractal Objects
Mass Fractal Dimension = d
Real Space
M~Rd
Dispersion
d = 3
d = 2
M ~V ~ R3
M ~V ~ R2
M ~V ~ R1
M ~V ~ R2.2

## Slide 20: Surface Fractal Dimension
S ~ Rds
S ~ R2
fractal or self-affine surface
Sharp interface

## Slide 21: Porod Slope for Fractals
Structure
Scaling Relation
Porod Slope= ds – 2dm
dm = 3
d
S
= 2
- 4
dm = 3
2 < d
S
≤ 3
- 3 ≤ Slope ≤ - 4
1 ≤ ds = dm ≤ 3
- 1 ≤ Slope ≤ - 3
Smooth Surface
Rough Surface
Mass Fractal
I(q)=qds-2dm

## Slide 22: Scattering from colloidal aggregates
R
r
Precipitated Silica
Log q
Log I
qR = 1
qr = 1
q-d
q-4

## Slide 23: Morphology of Dimosil® Tire-Tread Silica
Two Agglomerate length Scales
Soft = Physically Bonded
Hard = Chemically Bonded
-2
-4
7 µm
116 µm
300 nm
Light Scattering
USAXS
126 Å
Dispersion
Reinforcement
Schaefer, D. W., Kohls, D. & Feinblum, E. Morphology of Highly Dispersing Precipitated Silica: Impact of Drying and Sonication. J Inorg Organomet Polym 22, 617–623 (2012).
Notes: ----- Meeting Notes (3/17/12 17:53) -----
Same light scattering data.

## Slide 24: Aggregates are robust
Soft Agglomerates
Hard Agglomerates
Aggregates
What is the ideal aggregate size?
shear
Ragg

## Slide 25: Exploring the Nanoworld
Tubes
Carbon Nanotubes
Sheets
Layered Silicates
How valid are the cartoons?
What are the implications of morphology for material properties?
Spheres
Colloidal Silica
1-d 2-d 3-d
Answers come from Small-Angle Scattering.
Schaefer, D.W. and R.S. Justice, How nano are nanocomposites? Macromolecules, 2007. 40(24): p. 8501-8517.

## Slide 26: The Promise of Nanotube Reinforcement
α = aspect ratio

## Slide 27: 0.01% Loading CNTs in Bismaleimide Resin
5000 Å
-1
)
q(Å
)
PD
LIGHT
-1
.00001
.001
10
SAXS
.1
Length
Diameter
Surface
Local
Structure
-1
-4
Intensity

## Slide 28: 0.05% Carbon in Bismaleimide Resin
2000 Å
d
Lp
Worm-like branched cluster

## Slide 29: TEM of Nanocomposites
Hyperion MWNT in Polycarbonate
Pegel et al. Polymer (2009) vol. 50 (9) pp. 2123-2132

## Slide 30: Don’t Believe the Cartoons
Tubes
Carbon Nanotubes
Sheets
Layered Silicates
Spheres
Colloidal Silica
1-d 2-d 3-d
Schaefer, D.W. and R.S. Justice, How nano are nanocomposites? Macromolecules, 2007. 40(24): p. 8501-8517.

## Slide 31: Conclusion
If you want to determine the morphology of a disordered material
use small-angle scattering.

## Slide 32: Scattering from Fractal Objects: Porod Slopes
d = Mass Fractal Dimension
ds = Surface Fractal Dimension
Match at qR = 1
qR = 1
Large q
~ Sv/q-x
Small q

## Slide 33: Differential Scattering Cross Section
sample
dΩ
θ = scattering angle
Plane wave J0
Spherical wave JΩ
Spherical wave: Flux JΩ = energy/unit solid angle/s or photons/ unit solid angle /s
Plane wave: Flux J0 = energy/unit area/s or photons/unit area/s

## Slide 34: What do we really measure?
length
Area
beam
Scattering cross section depends on sample size: Bad
Often called the scattering cross section or the intensity