## Slide 1: PDF Analysis
Thomas Proffen
tproffen@ornl.gov
Neutron Data Analysis & Visualization Division

## Slide 2: About me
PhD in Crystallography from Ludwig Maximilians Universität in Munich, Germany
Postdoc at the Australian National University in Canberra, Australia
Postdoc at Michigan State University
Instrument scientist at Los Alamos National Laboratory
Diffraction Group Leader at Oak Ridge National Laboratory (SNS and HFIR)
Director Neutron Data Analysis and Visualization at ORNL.
NPDF instrument at Lujan Center (LANL)
My car
Forschungsreaktor
München
NDAV Division

## Slide 3: The challenge : Knowing the ‘real’ structure
Traditional crystallographic approach to structure determination is insufficient or fails for
  Non crystalline materials
  Disordered materials: The interesting properties are often governed by the defects or local structure !
  Nanostructures: Well defined local structure, but long-range order limited to few nanometers (-> poorly defined Bragg peaks)
PDF to the rescue ...
S.J.L. Billinge and I. Levin, The Problem with Determining Atomic Structure at the Nanoscale, Science 316, 561 (2007).

## Slide 4: Total scattering ?
Cross section of 50x50x50 u.c. model crystal consisting of 70% black atoms and 30% vacancies !
Properties might depend on vacancy ordering !!

## Slide 5: Bragg peaks are blind ..
Bragg scattering: Information about the average structure, e.g. average positions, displacement parameters and occupancies.

## Slide 6: How about powder diffraction ?

## Slide 7: Finally the Pair Distribution Function
  The PDF is the Fourier transform of the total scattering diffraction pattern !
Proffen, Z. Krist, 215, 661 (2000)

## Slide 8: What is a PDF?
5.11Å
4.92Å
4.26Å
3.76Å
2.84Å
2.46Å
1.42Å
Pair distribution function (PDF) gives the probability of finding an atom at a distance “r” from a given atom.

## Slide 9
Simon Billinge
Emil Bozin
Xiangyn Qiu
Thomas Proffen
Example:
Local structure in LaxCa1-xMnO3

## Slide 10: LaMnO3: Jahn-Teller distortion
Mn-O bond lengths are invariant with temperature, right up into the R-phase
JT distortions persist locally in the pseudocubic phase
Agrees with XAFS result: M. C. Sanchez et al., PRL (2003).
Average structure
Local structure
Jahn Teller
Long Mn-O bond

## Slide 11
X. Qiu, Th. Proffen, J.F. Mitchell and S.J.L. Billinge, Orbital correlations in the pseudo-cubic O and rhombohedral R phases of LaMnO3, Phys. Rev. Lett. 94, 177203 (2005).
Refinement as function of
atom-atom distance r !

## Slide 12: LaMnO3: Simplicity of the PDF approach
30s
Distortions persist locally!
700 K data (blue) vs 750 K data (red)
Notes: This is a great plot. I think it would be stronger if you limited the range to say 15 so the Ir-Ir peak disappearance is amplified. It is in-your-face evidence…you don’t need to say any more. Forget the modeling, everyone will believe it if you just show the data! Well, don’t forget the modeling, put it in, but you get my meaning…really play this aspect up as it is great something like this can really be seen in the “raw” data.

## Slide 13: Software: Data modeling
PDFgui
Part of DANSE project.
http://www.diffpy.org/
Calculation and refinement of small model system (< 1000 atoms)
‘Rietveld’ type parameters: lattice parameters, atomic positions, displacement parameters, ..
New possibilities: Refinements as function of r range !
Automatic refinement of multiple datasets as function of T or x.
Intuitive GUI.
Engine pdffit2 can also be used in command mode.

## Slide 15: La1-xCaxMnO3: Phase diagram
Phase diagram draws itself from the parameters.
Unexpected detail emerges and demands interpretation.
FM
PI
Atomic displacement parameter (ADP) for Oxygen
(measure for thermal and static deviations from site)

## Slide 16: La1-xCaxMnO3: Phase diagram
Local structure
Average structure
Mn-O
long bond
ADP
Oxygen

## Slide 17
BES/Geosciences Program-Geochemical Equilibria and Reaction Dynamics: Atomic- to Pore-Scale Processes (ERKCC72)
H.-W. Wang1, D. J. Wesolowski1, T. E. Proffen2, A. I. Kolesnikov2, L. Vlcek1, W. Wang3, M. Feygenson2, J. O. Sofo4, L. F. Allard Jr.5, and L. M. Anovitz1
Example
Investigation of the structure and stability of SnO2 nanocrystal and its surface-bound water

## Slide 18
MD and PDF
MD: hydration layer only
L1 +L2 +L3 : 41 x 41 x 8 Å3
L1 +L2 : 41 x 41 x 6 Å3
L1 : 41 x 41 x 2.5 Å3
PDF for nonhydroxylated and hydroxylated models:
Box size: 41 x 41 x 23 Å3 ; 2592 atoms; # density = 0.068 Å-3; Uiso = 0.003 Å2;
1st coord. shell - 1:O-D; 2:D-D; 3:Sn-O; 4/5/6:O-O and Sn-Sn (c axis);
2nd coord. shell - 7/8:Sn-Sn, Sn-O, and O-O; 9: Sn-Sn (a and b axes)
MD: SnO2 + hyd. layer (hydroxlated model)
0.068
2
1
Observed PDF
0.068
0.084
1
3
4
5
6
7
8
9
Notes: HUMP…..
Nonhydroxylated model not as consistants with PDF because of D-D peak.

## Slide 19
850 ºC
22 ºC
PDF in-situ dehydration (cont.)
19
9.49%
2.65%
1.61%-Cl ; 1.04%-O
TGA
Notes: Distorted model to describe any related surfaces modifications, including loss of O, Cl, misorientation, twinning and microstrains arises from grain growth.

## Slide 20
Example:
“Complete” structure of
Gold Nanoparticles
Katharine Page
Ram Seshadri
Tony Cheetham
Thomas Proffen

## Slide 21: Gold nanoparticles
Nanoparticles often show different properties compared to the bulk.
Difficult to study via Bragg diffraction (broadening of peaks).
PDF reveals “complete” structural picture – core and surface.
This study:
  5nm monodisperse Au nanoparticles
  1.5 grams of material
  Neutron measurements on NPDF
50 nm
2nm

## Slide 22: Gold nanoparticles: First NPDF data
Bulk gold
Gold nanoparticles
Average diameter ~3.6nm
K.L. Page, Th. Proffen, H. Terrones, M. Terrones, L. Lee, Y. Yang, S. Stemmer, R. Seshadri and A.K. Cheetham, Direct Observation of the Structure of Gold Nanoparticles by Total Scattering Powder Neutron Diffraction, Chem. Phys. Lett. 393, 385-388 (2004).

## Slide 23: Nanoparticles: Particle size
Nanogold
Instrument resolution
Spherical particle envelope

## Slide 24: Modeling Au structure only
300 K: Rw = 33.8 %
scale = 0.2121(5)
a = 4.0753(1)
uiso(Au) = 0.01267(6)
δ1 = 1.980(7)
d = 26.13(7) Å
15 K: Rw = 27.8 %
scale = 0.2070(4)
a = 4.06515(5)
uiso(Au) = 0.0044(2)
δ1 = 2.257(5)
d = 25.54(4) Å
This is the conventional PDF nanoparticle approach… no ligand modeling.

## Slide 25: Modeling Au structure & ligand
U N C L A S S I F I E D
+
CF3(CF2 )5(CH2 )2S-
300 K: Rw = 31.4 %
scale (Au) = 0.2082(5)
scale (molecule) = 0.0485(6)
a (Au) = 4.0755(1)
a(molecule) = 49.40(3)
uiso(Au/molec) = 0.01227(5)
δ1 (Au) = 1.953(7)
srat (molecule)= 0.02(3)
15 K: Rw = 24.7 %
scale (Au) = 0.2054(4)
scale (molecule) = 0.0604(6)
a (Au) = 4.06500(5)
a(molecule) = 49.23(2)
uiso(Au/molec) = 0.00433(2)
δ1 (Au) = 2.256(6)
srat (molecule)= 0.03(14)
~1 Mol./110 Å2 particle surface
Au-S

## Slide 26: Modeling of nanoparticle data - future !
Using DISCUS/DIFFEV
http://discus.sourceforge.net/
Approach: The particle is modeled as a whole.
Current work on gold nanoparticles: An fcc Au particle is constructed in DISCUS, we select a cuboctahedron.
Ligands (with ‘internal’ structure as constructed with DFT minimization) are located randomly at the particle surface with a defined surface density and defined Au-S distance, orientated out from the particle center.
Evolutionary algorithm is used to refine model parameters above (CPU intensive).
Oxford University
Press, October 2009

## Slide 27: Nanoparticle builder
Page, K., Hood, TC, Proffen, T, Neder, RB, J. Appl. Cryst., 44 (2), 327 - 336 (2011)

## Slide 28: Initial results (in progress ..)
Things to consider
Particle size distribution
Variations in ligands
Ligand-ligand interactions ?
Ligand floppiness
...
r(A)

## Slide 29
Experimental
Considerations

## Slide 30: How to obtain high quality PDFs ?
The PDF (similar to the Patterson) is obtained via Fourier transform of the normalized total scattering S(Q):
Requirements to obtain ‘good’ PDF:
High maximum momentum transfer, Qmax.
High Q-resolution.
Good counting statistics @ high Q.
Low instrument background
Where ?
Synchrotron sources or Spallation Neutron Sources
(high energy X-rays) (reactor neutron energies are too low)

## Slide 31: NPDF: the key to high quality, high r PDFs
The PDF (similar to the Patterson) is obtained via Fourier transform of the normalized total scattering S(Q):
Requirements to obtain ‘good’ PDF:
High maximum momentum transfer, Qmax.
High Q-resolution.
Good counting statistics @ high Q.
Low and stable instrument background.

## Slide 32: Q resolution ..

## Slide 33: Instruments at SNS for PDF studies

## Slide 34: MgCo – the power of neutrons and x-rays
 | bi for x-ray | bi for neutron
Mg | 12 | 3.631
Co | 27 | 0.779
PDF peak intensity ∝
where bi is the scattering length of the ith atom.
bmbn | Mg-Mg | Mg-Co | Co-Co
x-ray | 144 | 324 | 729
neutron | 13.18 | 2.83 | 0.607
NOMAD users have access to x-ray PDF measurements through ORNL-APS partner proposal.

## Slide 35: Reverse Monte Carlo
RMCprofile
  Atomic configurations ~600 to 20000+ atoms
  Fit both X-ray and neutron F(Q)
  Fit G(r)
  Fit Bragg profile (GSAS ToF 1-3)
  Polyhedral restraints
  Coordination constraints
  Closest approach constraints
Produce a static 3-D model of the structure (a snap-shot in time)
Link: http://www.isis.rl.ac.uk/RMC

## Slide 36: Summary
Analysis of total scattering gives valuable insight in structure  properties relationship
High-resolution instruments open the door to medium-range order investigations
Obtain structural information from disordered crystalline, amorphous of composite materials
Use multiple data sets (e.g. x-ray and neutron data) to characterize complex materials
http://totalscattering.lanl.gov
Th. Proffen