## Slide 1: An Introduction to Small-Angle Scattering
William T. Heller
EQ-SANS Lead instrument Scientist
Biology and Soft Matter Division (BSMD)
National School on Neutron and X-ray Scattering

## Slide 2: Outline
What is SAS and what can it do for you?
Basic concepts of the technique
SANS instrumentation
Planning a SAS experiment and data reduction
SAS data analysis and interpretation

## Slide 3: SAS
SAS is a tool for structural characterization of materials
  X-rays, neutrons and laser light can be used for SAS
One of the most widely applicable structural characterization techniques
  Solids, liquids, gasses
  Amorphous, crystalline or anything in between
  Pretty much any kind of material

## Slide 4: SAS applications A to Z
Alzheimer’s disease, aerogel, alloys
Bio-macromolecular assemblies, bone
Colloids, complex fluids, catalysts
Detergents, dairy (casein micelles)
Earth science, emulsions
Fluid adsorption in nanopores, fuel cells, food science (chocolate)
Gelation, green solvents
High pressure, high temperature…, hydrogen storage, helium bubble growth in fusion reactors
Implants (UHDPE)
Jelly
Kinetics (e.g. of polymerization or protein folding), keratin
Liquid Crystals
Magnetic flux lines, materials science
Nano-anything
Orientational order
Polymers, phase behavior, porosity
Quantum dots (GISAXS)
Rubber, ribosome
Soft matter, surfactants, switchgrass
Time-resolved, thermodynamics
Uranium separation
Vesicles, virus
Wine science
Xylose isomerase
Yttrium-stabilized zirconia (YSZ)
Zeolites
…anything?
Pretty close!

## Slide 5: Difference between SAS and Microscopy
incident
beam
Sample
Image
focusing optics
Detector
Sample
incident
beam

wavelength λ
scattering angle
Microscopy uses lenses to resolve a real-space image of the sample
SAS measures the interference of waves
Fourier space!
Averaged over volume!

## Slide 6: SAS is related to diffraction
Wave vector k: |k| = k = 2p/l
q in nm-1 or Å-1
ko
k
ko
k
q
J
q
q
d
q q
D = 2d sin(q)
2q = J
if D = n l then reflection, else extinction
Bragg: waves with wavelength l reflected by sets of lattice planes

## Slide 7: SAS probes density differences
Incoming waves scatter off the electron cloud (x-rays) or nuclei (neutrons)
Interference of scattered wavelets from the material adds up to a “net scattering” amplitude
  Fourier transform of the structure.
Measured intensity is the magnitude square of the amplitude.

## Slide 8: SAS – SAXS and SANS
X-rays
No charge
No mass
Interacts with electrons
Interaction varies with atomic number
Neutrons
No charge
Has mass
Interacts with atomic nucleus
Has spin
Interaction is a property of the nucleus
Cs
Zr
Mn
S
O
C
D
H
The fundamental physics of x-ray and neutron scattering don’t really differ, but their properties differ a great deal

## Slide 9: SAS – SAXS and SANS
X-rays
Readily available
  Lab-based sources
  Synchrotrons
Massive fluxes possible
  Time-resolved studies
  Extremely precious material
Neutrons
Large user facilities only
  Spallation sources
  Reactors
No radiation damage
Contrast variation
There are many experiments that really don’t require the use of neutrons.
SAXS and SANS are very closely related and provide directly complementary information
The choice between x-rays and neutrons is dictated by the problem

## Slide 10: SAS Instrumentation
SAS instruments are conceptually simple
Source: x-ray generator, synchrotron, spallation source or reactor
Monochromator/Chopper: Defines wavelength(s)
Collimating Optics: Defines the angular divergence of the beam
Determines the maximum size probed
Detector: Collects the radiation scattered by the sample
Large detectors provide better angular coverage

## Slide 11: SAS Instrumentation
HFIR guide hall a few years ago

## Slide 12: SAS Instrumentation
The neutron wavelength is related to its momentum
De Broglie:
The wavelength-velocity relationship enables time-of-flight neutron scattering techniques

## Slide 13: SAS measurements
A SAS measurement, once properly reduced, provides the scattering cross section per unit volume
Io
dI
dW
D
dI/dW = Scattered intensity per solid angle
Io = Primary beam intensity
T = Transmission (x-ray absorption, incoherent neutron scattering)
D = Thickness
dS/dW = Scattering cross section per unit volume [cm-1sterad-1]
[cm-1sterad-1]
SANS instruments more commonly provide reduced data in absolute units (1/cm) than SAXS instruments

## Slide 14: SAS measurements
Plan your experiment well!
  What Q-range would I like, and what must I have?
  How large is each sample?
  How much material do I need?
  For how long should I measure my samples?
  How can I optimize my sample quality?
  What control measurements do I need to perform?
  How will I reduce my data?
  Less is often more: Do fewer things but those do right! (especially with neutrons)
  Ask your local contact / instrument scientist for advice well ahead of time!

## Slide 15: SAS Measurements
Normalization to monitor or time
Background data sets
Sample transmission
Azimuthal averaging
Absolute intensity scale (cm-1)
Measure and subtract background very carefully!
Do the absolute intensity calibration – it’s worth the extra effort!

## Slide 16: SAS Analysis
Analyzing SAS data is far harder than taking SAS data
Model fitting is complicated by the sheer number of models available for fitting the data
Be patient and be prepared to explore
Bruce McCandless II took the first untethered space walk in February 1984. Here we see him from Challenger, floating above Earth.
If you feel like you are floating off in the middle of nowhere, you are neither the first, nor will you be the last, SAS practitioner to feel that way

## Slide 17: Scattering from Particles
Discreet particles are often the easiest to understand
is the number density of particles
is the form factor (particle shape)
is the structure factor (particle interactions)

## Slide 18: Form Factors
Sphere
Ellipsoid of Revolution
Long & Thin cylinder
Polymer coil

## Slide 19: Structure Factor
S(q) examples: hard sphere potential, sticky sphere, screened coulomb etc.
S(q)·P(q) is not always valid and useful!

## Slide 20: Guinier Analysis
At small q, anything that could reasonably be considered a discrete object follows Guinier’s approximation.
Modified Guinier approximations exist to determine cross sectional radius of rods or thicknesses of sheets
100 Å radius
~77.46 Å Rg

## Slide 21: Guinier Analysis
Precise Rg is 77.46 Å
Guinier fitting can be applied to scattering data from discreet particles regardless of the shape of the particle

## Slide 22: Pair Correlation Function Analysis
Dmax
r
  P(r) : inverse Fourier transform of scattering function : Probability of finding a vector of length r between scattering centers within the scattering particle.
P(r) provides some indication of particle shape
Dmax

## Slide 23: Example: A Protein Complex
Protein Kinase A is an important regulatory protein complex that phosphorylates proteins in response to a cellular signal
SAXS and SANS with contrast variation, when combined with structural modeling, made it possible to construct a model that shows how the subunits in the complex assemble into the holoenzyme
Blumenthal, et al., J. Biol. Chem 289: 28505-28512 (2014).

## Slide 24: Example: Proteins in a Porous Material
Entrapment of bio-macromolecular assemblies: bio-composite, biomimetic, bio-inspired for catalysts, sensors, functional materials – for example light harvesting antenna complexes for solar energy
SANS with contrast variation shows structure of proteins in a complex gel matrix
Luo, et al., ACS Appl. Mater. Interfaces 1: 2262-2268 (2009).

## Slide 25: Hierarchical Structures
Structural information viewed on five length scales. Structural features at larger length scales are observed at smaller Q.
Scattering analysis that describes hierarchical structures: Mass Fractal (Teixeira), Unified Fit (Beaucage) combine power law scattering ranges with Rg transitions
Adapted from DW Schaefer MRS Symposium Proceeding 1987

## Slide 26: Example: Biomass to Cellulosic Ethanol “grass to gas”
Hydrolysis
Cellulase enzyme
4 X 14 nm
Pretreatment
Cell wall
100 nm
Adapted from DOE GTL image gallery (genomics.energy.gov)
Fermentation
The challenge: structural complexity!
Feedstock
Switchgrass
Poplar
Corn Stover

## Slide 27: Dilute Acid Pretreatment of Switchgrass
Treated
SEM
SANS of Switchgrass in D2O
Structural
Change Onset
Elementary Cellulose Fibril
Cross-sectional View
Q-4
D
Pingali, et al., Biomacromolecules 11: 2329-2335 (2010).

## Slide 28: Non-particulate Scattering

## Slide 29: SAS Summary
SAS probes length scales from 1nm to 100nm
SAS does not see atoms, but larger, interesting features over many length scales
SAS is similar to diffraction but does not require crystals
SAS applications are only limited by imagination
SAS can be used alone, but often complementary to other methods, such as microscopy, NMR
SAS data analysis is application dependent, using a diverse set of approximations, models and software

## Slide 30: Further Reading
Guinier, A., Fournet, G. 1955. Small-Angle Scattering of X-rays. John Wiley & Sons, New York. The classical work on SAS. The book focuses on x-rays, but the theory and data interpretation also applies to SANS.
Roe, R. J. 2000. Methods of X-Ray and Neutron Scattering in Polymer Science. Oxford University Press, New York and Oxford. This book covers the basic scientific principles of SAS thoroughly and is suitable for the non-expert.
Higgins, J. S., and Benoît, H. C. 1994. Neutron Scattering from Polymers. Clarendon Press, Oxford. A comprehensive description of neutron scattering, particularly SANS, that is focused on polymers. It is very useful for anyone interested in SANS.
Pedersen, J. S., 1997. Analysis of small-angle scattering data from colloids and polymer solutions: modeling and least-squares fitting. Adv. Colloid Interface Sci. 70:171-210. Contains a comprehensive list of form factors and structure factors that are used for interpreting SAS data.
Urban, V. S., 2012. Small-Angle Neutron Scattering. In: Characterization of Materials, edited by Elton N. Kaufmann. Copyright 2012 John Wiley & Sons, Inc. A concise introduction to theory and practical considerations of SANS.